## Slide 1
Lecture Series: Thermodynamics of polymer blends and solutions
Pierre J. Walker

## Slide 2: Overview
Flory–Huggins Equation
  Derivation
  Stability and Equilibrium
  Criticality
  Application
Polymer solutions
  Dilute mixtures
  Semi-dilute solutions
Beyond Flory–Huggins
  Alternative theories
  Polyelectrolytes
  PEO+IL system

## Slide 3
Flory–Huggins Equation

## Slide 4: Derivation of Flory–Huggins
For a pure species , we can write:
  : Translational entropy
  : Configurational entropy of an ideal chain
  : Residual energy from all other interactions
In a mixture:

## Slide 5: Derivation of Flory–Huggins
It is more practical to express as a mixing function:
  Define volume fractions: assumes

## Slide 6: Derivation of Flory–Huggins
It is more practical to express as a mixing function:
  Define volume fractions: assumes
  Further assume all monomers are the same size, :

## Slide 7: Derivation of Flory–Huggins
It is more practical to express as a mixing function:
  Define volume fractions: assumes
  Further assume all monomers are the same size, :
The first term is the mixing entropy:

## Slide 8: Derivation of Flory–Huggins
It is more practical to express as a mixing function:
For the second term, we can write:
  Where:
  The leading order terms must be :

## Slide 9: Derivation of Flory–Huggins
It is more practical to express as a mixing function:
For the second term, we can write:
  Where:
  The leading order terms must be :
It corresponds to the mixing energy:

## Slide 10: Derivation of Flory–Huggins
The parameter has a lot of heavy lifting to do…
  Accounts for excluded volume, van der Waals interactions, hydrogen bonding, conformational changes, etc.
If we assume some binding energy per site between species and :
  From A’s perspective, A sites were replaced with B:
  Similarly, from B’s perspective:
  The total excess energy is then:
  We can write :
A
B
A
B
A

## Slide 11: Derivation of Flory–Huggins
This simplified expression lets us interpret
  If A and B have favourable interactions, then:
  If A and B have unfavourable interactions:
  Broadly speaking,
Typically, will be expressed as a correlation:
  is the ‘entropic’ contribution
  is the ‘enthalpic’ contribution

## Slide 12: Derivation of Flory–Huggins
We now have a complete free energy expression:
How do we use it?

## Slide 13: Stability and Equilibrium
The system will always try to minimize the free energy:
Stable
Metastable
Unstable
Local state variable

## Slide 14: Stability and Equilibrium
The system will always try to minimize the free energy:
For Flory–Huggins:
Why doesn’t the system approach the lowest value of ?
We have fixed
In a stable phase:

## Slide 15: Stability and Equilibrium
The system will always try to minimize the free energy:
For Flory–Huggins:
Why doesn’t the system approach the lowest value of ?
We have fixed
In a stable state:
In a metastable / unstable state:

## Slide 16: Stability and Equilibrium
The system will always try to minimize the free energy:
For Flory–Huggins:
Why can a metastable exist?
The system can’t ’see’ the full landscape
Fluctuations allow it to see nearby states
From statistical mechanics: a

## Slide 17: Stability and Equilibrium
The system will always try to minimize the free energy:
For Flory–Huggins:
Why can a metastable exist?
The system can’t ’see’ the full landscape
Fluctuations allow it to see nearby states
From statistical mechanics: a
The closer we get to the unstable region, the larger becomes
When , ,
It can now ‘see’ the full landscape (and the global minimum)

## Slide 18: Stability and Equilibrium
The system will always try to minimize the free energy:
For Flory–Huggins:
We can now define the spinodal for this system:
For Flory–Huggins:
Unstable
Metastable
Metastable
Stable
Stable

## Slide 19: Stability and Equilibrium
The system will always try to minimize the free energy:
How do we define the binodals?
For , we want to find and which: where is the phase fraction
We must maintain mass-balance:
Adding a Lagrange multiplier:

## Slide 20: Stability and Equilibrium
Taking derivatives:
  From :
  From :
  From :
  From :
Re-arranging:
Equality of chemical potential
Equality of osmotic pressure

## Slide 21: Stability and Equilibrium
Taking derivatives:
  From :
  From :
  From :
  From :
Re-arranging:
Equality of slopes
Equality of intercepts
Definition of a common tangent line!

## Slide 22: Stability and Equilibrium
Re-arranging:
What happens as we vary ?

## Slide 23: Criticality
Definition for a critical point:
  Fluctuations are infinite:
  Must be an extremum:
For Flory–Huggins:

## Slide 24: Criticality
Definition for a critical point:
  Fluctuations are infinite:
  Must be an extremum:
For Flory–Huggins ():

## Slide 25: Criticality
Definition for a critical point:
  Fluctuations are infinite:
  Must be an extremum:
For Flory–Huggins ():

## Slide 26: Application
Returning to the correlation for :
Compared to the expression for :
We can obtain different types of phase behaviour depending on and :
  , with , leading to UCST behaviour
  , with , leading LCST behaviour (for some chain lengths)

## Slide 27: Application
Despite its approximations, the Flory–Huggins expression does a remarkable job reproducing experimental results:
Its simple form also allows for easy implementation in other theories like Cahn–Hilliard:

## Slide 28: Summary
We derived the Flory–Huggins equation:
  First term accounts for changes in translational entropy
  Second term accounts for all other excess interactions:
Conditions for spinodal:
Conditions for binodal: and
Critical point: and

## Slide 29
Polymer Solutions

## Slide 30: Dilute Mixtures
Take the case where :
The Osmotic pressure is defined as:
Using
X

## Slide 31: Dilute Mixtures
Take the case where :
The Osmotic pressure is defined as:
Using
X

## Slide 32: Dilute Mixtures
Take the case where :
The Osmotic pressure is defined as:
Using
X

## Slide 33: Dilute Mixtures
Take the case where :
The Osmotic pressure is defined as:
Using
X

## Slide 34: Dilute Mixtures
Take the case where :
The Osmotic pressure is defined as:
Giving:
  The excluded volume:
  Three-body interaction:
X

## Slide 35: Dilute Mixtures
For a polymer solution (, ):
Interpretation:
  For very low compositions (van’t Hoff’s law): Each chain will contribute to
  When , energetic and entropic contributions perfectly cancel, leading to ideal chain behaviour
  For , increases due to favourable interactions between solvent and chain (good solvent).
  Gives an experimental method to determine !
X

## Slide 36: Semi-Dilute Solutions
For a polymer solution (, ):
In a good solvent, with increasing concentration, the second term will dominate:
  Osmotic pressure is independent of molar mass ✔️
  This mean-field theory predicts that the semi-dilute regime is reached when: which is a very low concentration…
  It also gets the scaling of with wrong…

## Slide 37: Semi-Dilute Solutions
For a polymer solution (, ):
The primary mistake that Flory–Huggins makes is assuming a uniform distribution of monomers in solution
  Ignores correlations between monomers
At what concentration does the excluded volume matter?
  We know for a single chain with excluded volume in a good solvent:
  Chains will begin to overlap when:

## Slide 38: Semi-Dilute Solutions
For a polymer solution (, ):
We define the semidilute regime when
In this regime, there will a number of monomers which act as if they are a single chain ():
  The correlation length is then defined as:
  The concentration of monomers in this volume will match the actual concentration of the solution:

## Slide 39: Semi-Dilute Solutions
The chain formed from blobs of size behave as if they are in a melt
The size of the chain can then be written as:
  Return to the ½ scaling!
With increasing , we will see changes in slope for the polymer size
Note that decreases with , but doesn’t.
  When , we will have reached the concentrated regime:
Semi-dilute regime:

## Slide 40: Semi-Dilute Solutions
We still want an expression for in the semi-dilute regime.
Using de Gennes scaling theory:
  At , we want the limiting behaviour to follow van’t Hoff’s law:
  Use a power law form:
  Substitute :
  We know :
  Giving:

## Slide 41: Summary
Osmotic pressure is the when a membrane separates a solute from the pure solvent
From Flory–Huggins:
  The excluded volume:
  Three-body interaction:
  Theta-point is when
In the dilute limit ():
In the semi-dilute limit ():
  Flory–Huggins misses-out on monomer-monomer correlations
  Osmotic pressure:

## Slide 42
Beyond Flory–Huggins

## Slide 43: Alternative Theories
The parameter abstracts away a lot of the physics:
  What leads to LCST / looping behaviour?
UNIFAC-FV provides an improvement to FH:
  Fitting to smaller molecules allows UNIFAC to extrapolate to longer chains
  Still more of a correlation…
SAFT-type equations provide a separation of contributions:
  Can better understand the physics of what leads to LCST / looping behaviour
assoc. > disp.
assoc. < disp.
assoc., disp. < id.

## Slide 44: Polyelectrolytes
One interaction that cannot be capture by is electrostatics…
Voorn and Overbeek (1957) included the simplified equation of Debye–Hückel to account for the electrostatics:
  Can predict polyelectrolyte coacervation
  Incorrectly predicts positive tie-lines
  Cannot predict re-entrant behaviour
  Limiting assumptions:
    Low ionic strength
    Ignores configurational entropy when forming chains of charged monomers

## Slide 45: Polyelectrolytes
Based on the MSA theory by Blum (1977), Zhang and Wang (2017) developed liquid state theory:
  Starts from a hard-sphere reference (excluded volume)
  Include electrostatics with a more-accurate theory
  Account for the entropy change from forming chains
Substantial improvements on Voorn–Overbeek:
  Correct tie lines
  Re-entrant behaviour
  Reproduce experimental results
+
+
+
+
+
-
-
-
-
-
+
+
+
+
+
-
-
-
-
-

## Slide 46: PEO+IL System
PEO+IL is an interesting system:
  Hydrophilic chain
  Hydrophobic (ish) ‘solvent’
  Would expect UCST behaviour, skewed towards pure solvent
  Reality: centered LCST(?)
Explaining the LCST:
  PEO and EMIM will experience some hydrogen bonding:

## Slide 47: PEO+IL System
Explaining the location of the LCST is harder:
  Flory–Huggins and most other theories would agree the LCST should be skewed
  Most previous theories argue that the change is due to aggregation of ILs into larger molecules:

## Slide 48: PEO+IL System
The clustering argument has some flaws:
  Large clusters only form when there is a high enough IL concentration
  The addition of PEO will disrupt the cluster formation
What if it’s just the electrostatics?
  Taking a very simplified model
  For a symmetric system (), starts off on the polymer side!
  Increasing the chain length does push the critical point back to the IL side
  In the PEO+IL system,

## Slide 49: PEO+IL System
The critical scaling also changes
  In Flory–Huggins:
  In this system, both have a scaling of

## Slide 50: Future Work
‘Complete’ model for PEO+IL
  Include PEO-IL association for the LCST behaviour
  Must include electrostatics to account for the shift in LLE
Further study of the critical behaviour:
  What happens when you include in the theory?
  For sufficiently large , will we recover the original scaling?